Supplementary Material for "Heat capacity and other thermodynamic properties of hcp-CrH and hcp-CrD"

Mikhail A. Kuzovnikov a,, Vladimir E. Antonov b, Valery I. Kulakov b, Radion I. Usmanov b,c

a Centre for Science at Extreme Conditions and School of Physics and Astronomy,

University of Edinburgh, Edinburgh EH9 3FD, United Kingdom

b Institute of Solid State Physics RAS, 142432 Chernogolovka, Moscow District, Russia

c National Research University Higher School of Economics, 20 Myasnitskaya ul., 101000 Moscow, Russia

Fig. S1. Density Nel of electronic states in hcp-CrH calculated by DFT in this paper. Filled states below the Fermi energy EF = 0 are highlighted in yellow.

Fig. S2. Plot of CV/T vs. T2 for hcp-CrH. The red curve shows the dependence calculated in this paper. The green line is a linear fit to this dependence at T2 < 50 K2. The blue curve is the β·T3 dependence with the experimental value of β = 0.042 mJ/K4/mol CrH obtained previously [16] for an hcp-CrH sample prepared by the electrochemical method.

Some of the results obtained in the paper are additionally presented in digital form:

File “g(E) of CrH and CrD.dat” contains the spectra g(E) of phonon density of states for hcp-CrH and hcp-CrD plotted in Fig. 5. The optical part goptCrH(E) of the spectrum for CrH is taken from Ref. [3]; the goptCrD(E) for CrD is calculated as 1.43goptCrH(E⋅1.43); the acoustic parts gacCrH(E) and gacCrD(E) are calculated with the density-functional theory (DFT). The areas under the gac(E) and gopt(E) curves are set equal to 3 phonon modes each.

File “Delta Cpv for CrH.DAT” contains the calculated temperature dependences of the coefficient αV of thermal expansion, molar volume V, bulk modulus B0, and the difference ΔCPV = αV2TVB0 between CP and CV for hcp-CrH. The dependences are plotted in Fig. 8.

File “Cp and Cv for CrH and CrD.DAT” contains the calculated temperature dependences of CV and CP for hcp-CrH and hcp-CrD. Graphs of these dependencies are presented in Fig. 3 and Fig. 9, respectively.

File “DeltaG0 for CrH.DAT” contains the calculated temperature dependences of standard (at P0 = 1 atm) Gibbs free energy GCrH0of hcp-CrH, GCr0of bcc-Cr, and (12)GH20 of gaseous hydrogen and the Gibbs free energy ΔG0=GCrH0−GCr0−(12)GH20. The ΔG0(T) dependence determined in this way may differ by a constant from the Gibbs energy of the reaction Cr + (1/2)H2 → CrH. The dependences are plotted in Fig. 12 by solid curves.

File “DeltaG0 for CrD.DAT” contains similar dependences calculated for hcp-CrD. The dependences are plotted in Fig. 12 by dashed curves.

File “Peq and DeltaG0eq for CrH.DAT” contains the calculated temperature dependence of the Gibbs energy ΔGeq0 of the reaction Cr + (1/2)H2 → CrH and the temperature dependence of the pressure Peq of the phase equilibrium Cr + (1/2)H2 = CrH. The dependences are shown in Fig. 13 and Fig. 14, respectively, by thick solid green curves.

Corresponding author. Centre for Science at Extreme Conditions and School of Physics and Astronomy, University of Edinburgh, Edinburgh EH9 3FD, United Kingdom.

E-mail address: m.kuzovnikov@ed.ac.uk (M.A. Kuzovnikov).